[image: image1.png]miller-stephenson product Information

‘www.miller-stephenson.com



[image: image2.png]miller-stephenson product Information

‘www.miller-stephenson.com




[image: image1.png][image: image2.png][image: image3.png]


[image: image3.png]

VertrelTM XF Cleaning Agent

MS-780 (Aerosol) NSN 6850-01-460-4914

MS-782 (Bulk Liquid)

MS-780 and MS-782 are a hydrofluorocarbon fluid which is ideally suited for medical applications involving cleaning and rinsing, water dispersion, particulate removal, fluorocarbon lubricant cleaning, and oxygen service cleaning.  Unique physical properties include high density, low viscosity and low surface tension, making it ideal for cleaning light oils and particulate matter from metal and non-metal parts.. 

ADVANTAGES:
· Evaporates quickly
· Leaves no residue
· Nonflammable
· Compatible with most plastics, elastomers and metals
· Chemical and thermal stability
· Non ozone depleting
· Volatile organic compounds: exempt

· NSN 6850-01-460-4914 (Aerosol)

· RoHS Compliant
VERTREL™ XF PHYSICAL PROPERTIES:

(Measured @ 77°F, unless otherwise noted)

Liquid density…………………………………………1.58 g/cc

Boiling point………………………………………..130°F/55°C

Vapor pressure………………………………………226 mmHg

Surface tension……………………………………..14.1 dyn/cm

Viscosity………………………………………………..0.67 cPs 

Heat of vaporization……………………..31.0 cal/g at boiling pt.

Specific heat at 68°F/20°C…………………….…..1.13 kJ/kg°C

Plastic Compatibility:

(Immersion: 15 Minutes at Room Temperature)

Polyethylene
Acetal

Polyphenylene Oxide, PPO

Epoxy

Polyester, PET,PBT

Liquid Crystal Polymer

Polyimide, PI,PEI,PAI

Phenolic

Polyetherketone, PEK

PTFE, ETFE

Polyaryletherketone, PEEK

CPVC, PVC

Polyarylsulfone

 
Ionomer

Polypropylene


Polysulfone

Polyphenylene Sulfide, PPS

Polystyrene

ABS

Note: Test for compatibility before use. 
Elastomer Compatiblity:

(Immersion: 15 minutes at Room Temperature)

Buna N, NBR, Nitrile
Buna S, SBR, GRS

Butyl Rubber, IIR


Chlorosulfonated PE

EPM, EPDM


Polysulfide

Natural Rubber, Isoprene

Neoprene

Urethane



Viton®
Silicone

Note: Test for compatibility before use.

Metal Compatibility:

(2 weeks at  212°F 100°C in sealed tubes)
Zinc1


Aluminum

Stainless Steel

Copper1

Brass1
Vertrel™ XF is not compatible with strong bases; therefore, contact with highly basic process materials is not recommended.

1Slight discoloration with water present.

Note:  Test for compatibility before use.

Safety Data Sheets (SDS) are available upon request.
1342-4K


